- Specifications

| Nominal Voltage | 12V |
| --- | --- |
| Rated Capacity 770F(250C) (20HR) | 5.0Ah |
| Dimensions (mm) | Length | 90±1.5 |
|  | Width | 70±1.5 |
|  | Height | 100±2 |
|  | Total Height | 106±2 |
| Approx. Weight (kg) | 1.54±3% |
| Terminal | T1 |

- Characteristic

| Capacity 770F(250C) | 20HR (0.250A) | 5.00Ah |
| --- | --- | --- |
|  | 10HR (0.465A) | 4.65Ah |
|  | 5HR (0.850A) | 4.25Ah |
|  | 1HR (3.050A) | 3.05Ah |
|  | 15 min rate (9.25A) | 2.31Ah |
| Internal Resistance | Full Charged Battery 770F(250C) | Approx. 35mΩ |
| Temperature dependence of capacity (20HR) | 1040F(400C) | 102% |
|  | 770F(250C) | 100% |
|  | 320F(00C) | 85% |
|  | 50F(-150C) | 65% |
| Self-Discharge 680F(200C) (Capacity after) | 3 months | 90% |
|  | 6 months | 80% |
|  | 12 months | 60% |
| Max. Discharge Current, 770F(250C) | 75A(5s) |
| Floating design life, 770F(250C) | 5 years |
| Constant Voltage Charge,770F(250C) | Cycle | 14.5~14.9V(-24mV/0C) max. current: 1.5 A |
|  | Float | 13.6~13.8V(-18mV/0C) |

| Constant Current Discharge Characteristics (A), 770F(250C) |
| --- |
| F.V/TIME | 5min | 10min | 15min | 30min | 60min | 2H | 3H | 5H | 8H | 10H | 20H |
| 1.60V/cell | 19.00 | 12.00 | 9.25 | 5.00 | 3.17 | 1.79 | 1.31 | 0.880 | 0.585 | 0.480 | 0.258 |
| 1.70V/cell | 18.05 | 11.40 | 8.84 | 4.78 | 3.05 | 1.72 | 1.28 | 0.865 | 0.580 | 0.475 | 0.255 |
| 1.75V/cell | 17.70 | 11.15 | 8.68 | 4.68 | 3.00 | 1.69 | 1.25 | 0.850 | 0.570 | 0.465 | 0.253 |
| 1.80V/cell | 17.35 | 10.90 | 8.52 | 4.59 | 2.95 | 1.66 | 1.23 | 0.835 | 0.565 | 0.460 | 0.250 |
| Constant Wattage Discharge Characteristics (Watt), 770F(250C) |
| F.V/TIME | 5min | 10min | 15min | 30min | 60min | 2H | 3H | 5H | 8H | 10H | 20H |
| 1.60V/cell | 34.50 | 22.00 | 17.12 | 9.34 | 5.96 | 3.39 | 2.50 | 1.700 | 1.145 | 0.945 | 0.510 |
| 1.70V/cell | 33.10 | 21.10 | 16.49 | 9.00 | 5.80 | 3.29 | 2.47 | 1.685 | 1.140 | 0.940 | 0.505 |
| 1.75V/cell | 32.75 | 20.80 | 16.34 | 8.89 | 5.74 | 3.26 | 2.44 | 1.670 | 1.130 | 0.930 | 0.503 |
| 1.80V/cell | 32.40 | 20.55 | 16.19 | 8.80 | 5.70 | 3.23 | 2.42 | 1.655 | 1.120 | 0.920 | 0.500 |